5 STAGE WASH PRETREATMENT PARAMETERS

|  | Stage 1 | Stage 2 | Stage 3 | Stage 4 | Stage 5 |
| --- | --- | --- | --- | --- | --- |
| Products - Oakite | Inproclean / 1300 | Rinse | Cryscoat 547C | Rinse | 200 – 303 – 001 |
| pH Additive | N/A | Fresh water - Stage 4 overflow | Adjust OX -automatic Enprox 714 - manual | Fresh Water | N/A |
| Spray Zone | 12’ | 9’ | 9’ | 6’ | 6’ |
| Conc. - Target* | 3.5% | N/A | 2% | N/A | 1.25 |
| Conc. - Parameters** | 3 - 4% | Max. 0.6 | 1.5 - 2.5% | Max. 0.6 | .75 – 1.5 |
| pH - Target/Range | 8 - 10 pH° | Monitor | 4.75 pH/4.5 - 5.0 pH | Monitor | N/A |
| Temperature | 60 - 66C/140 - 150°F | Ambient | 49 – 54oC/120 – 130oF | Ambient | 43 - 52°C |
| Nozzle Pressure (PSI) | 25/30 | 15 | 17 | 15 | 10 |
| Tank Capacity (Litres) | 15,890 liters | 8,512 liters | 7,877 liters | 4,964 liters | 8895 liters |
| Litres to Charge | 556 liters | N/A | 157 liters | N/A | 111 liters |
| Maximum Line Speed | 6’/min. | 6’/Min. | 6’/min. | 6’/min. | 6’/min |
| Dump Schedule (TDS-PPM) | 4 - 6 months | Target TDS - 350 Max 530 PPM or Every Month | 4 - 6 months | Target TDS - 250 Max 530 PPM or Every Month | Max. 530 TDS |

*	“Target” is the optimum desired concentration.

**	“Parameter” is the maximum allowable variance of concentration.  Corrective action must be taken immediately when the concentration nears (depends on the stability of the solution) the parameter.  If the wash solution goes out of any of the above parameters contact the Supervisor immediately and take the appropriate corrective action.