LIQUID PAINT ON-LINE

INFORMATION RECORD SHEET

The following information is required whenever paint is put on-line to be mixed prior to painting:

All information must be recorded clearly and legibly.

- Batch number

This is to be recorded on the 8 digit batch number - No abbreviated forms.

- Barrel number

This is the hand written number or letter group on the ID label on the side of the barrel.

- Date and time On-line

This is the date and time the paint was put on-line to pre-mix.

- Color

To be recorded as the color of the paint.

- (C

To be recorded as (C of paint in barrel when put on - line/(C of paint when sprayed ( temperature at which viscosity is done at.  i.e.:  15(C/33(C (15(C is the paint in the barrel; 33(C is the spraying temperature).

Minimum temperature to put paint on-line:  15(C

Application temperature of the paint:  (31 - 36 (C)

Heaters are set at:  32(C

- Viscosity

To be recorded as the number of seconds using A Zahn #4 Cup.  See Liquid Paint Quality Assurance Procedure for specific operating procedure.

- Shift

Record shift letter (“A” or “B”)

- Initial

The initials of the individual who tested the barrel and/or put the paint line to pre-mix are required.

- Comments

- Use this section to add any helpful notes in regards to the paint.

|  | LIQUID PAINT ON-LINE INFORMATION SHEET |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| BATCH # | BARREL # | DATE | TIME ON-LINE | COLOUR | TEMP(*C) | VISCOSITY | SHIFT | EMP. # | COMMENTS |