SOUTH PAINT LINE

COLOUR CHANGE PROCEDURE

This procedure applies to the process required when changing colours in the paint booth.

A minimum of 20 feet and a maximum of 30 feet of empty track space are required.  This is to ensure that all parts painted the previous colour have exited the booth prior to painting the next colour.

After completing painting the current colour all guns and paint lines must be flushed out using gun wash.  Whenever flushing out - the air must be shut OFF and a face shield or painter hood must be worn.

If the changed colour is on-line (red, charcoal, green) then . . .

1.	Take gun tips off and soak them in a cup of thinner.  (Clean them before you replace them on the guns.

2.	Shut off the current paint lines.

3.	Turn on the thinner pump (located on the wall and also one in the front booth).

4.	Flush-out paint lines by opening the main thinner valve.  Flush lines until thinner are evident and colour is gone.

ALWAYS FLUSH OUT LINES INTO FLUSH BARRELS.  NEVER FLUSH OUT INTO WATER FALL TANK.

5.	Ensure all paint guns are clean.  (Follow coffee break flushing procedure on Painter’s Shift Checklist).

6.	Shut off main thinner valve.

7.	Flush in desired colour by opening the paint lines for that colour (ensure the paint is adequately agitated prior to pumping).

- Flush in until no thinner is present in the paint.

ALWAYS FLUSH IN FLUSH BARRELS - NEVER USE THE WATERFALL TANK.

8.	Put appropriate tips back on the guns, after cleaning with a toothbrush.

9.	Do not spray guns (testing pattern etc.) until the previous coloured parts have exited the booth!

10.	Shut thinner pump off.

ALWAYS KEEP AN EYE ON PAINT AND CATALYST GAUGES WHEN FLUSHING IN AND OUT TO BE SURE PRESSURE DOES NOT BUILD UP.  IF PRESSURE DOES BUILD UP, CHECK TO ENSURE AIR IS ON AT THE FEED PUMP AND/OR THAT PUMP IS RUNNING.  STOP THE PROCESS AND CONTACT YOUR  SUPERVISOR IF PRESSURE IS STILL BUILDING UP.

If the colour to be changed is not on-line then use the portable pump and . . .

1.	Mix the paint using the appropriate ratio of paint to catalyst.  Be sure to mix only enough to do the current job because once the paint is mixed it cannot be stored.  If needed some medium speed reducer can be added so the paint will spray better.

2.	Take gun tips off and soak them in a thinner cup.

3.	Flush-out the lines from the manifold to the paint guns using the thinner valve at the manifold.

4.	Using the portable pump hook up the guns and flush-in the colour.

5.	Clean tips with a toothbrush and thinner and put them back on the guns.

6.	Do not spray guns (testing pattern etc.) until the previous coloured parts have exited the booth!

When painting is complete all guns and paint lines used must be flushed out and the portable pump cleaned.

Do not begin spraying the second colour in any colour change until the previous colour has exited the booth.  This will help avoid colour contamination.