Polyurethane machine procedure

SAFETY:

- Read MSDS sheets for chemicals being used and understand hazards associated with each chemical.

- Be sure to wash your hands thoroughly after using a chemical because it could be hazardous to your health.

- Note any leaks from machine and bring them to supervisor’s attention.

- Follow the ‘Chemical Safety and Handling’ procedure, when operating the Polyurethane Machine.

OPERATION:

- Make sure day tanks are properly tagged.

- Use dry nitrogen blankets in tanks (pressurize 2-10 psi).  Keep the same pressures in both tanks.  (Keep lids closed when not filling tanks.)

- Ensure correct calibration after shift first starts and after lunch or supper.

- Do durometer checks after setup, after shift first starts, and after each break (plot on graph).

- Keep constant watch on pressures and temperatures.  If fluctuations occur, notify supervisor.

- Be aware:
a)  make sure machine goes through a purge cycle when pour cycle is complete.
b)  make sure nozzle is in purge barrel when purge cycle is initiated.

- Never run machine out of flush solvent.

- Never run machine in pour mode with solvent switch shut off.

- Never remove mixer cup without machine being shut off and locked out.

- Never attempt to remove day tank lids without relieving pressure in the tank being opened.

- Shut off nitrogen at the end of the production day.

- Relieve recirculation pressures at the end of the production day.

- Return tools when you are finished with them.  Practice good housekeeping at all times.