PROCEDURES TO REPAIR

OR REFINISH THE INTERIOR

OF SERVICE REPAINT

AIR SEEDER TANKS

A.	SURFACE PREPARATION

- All seeds, grains, chemicals, loose paint, oil, greases, and other foreign materials must be removed prior to painting.

Note:  It is recommended to use a high pressure washer and rinsed thoroughly, not leaving any soap residue.

- Dry surface thoroughly and prepare the damaged area using one of the following processes.

Note:  Tank must be grounded.

  - Light sandblasting

  - Mechanical grinders

  - Power sanding using 180 to 220 grit sandpaper

- Area should be wiped down with compatible solvent (SP05127T0).

- Metal must be treated using a metal conditioner.  As per Tank Paint Line Tank Repaint Procedure TPL202.

B.	APPLICATION: 	Refer to Product and Safety data material for more in-depth application and safety instructions.

Note:	Tank must be grounded

- The interior of the is now ready for painting:

  - Using EF74792P1/EF74792PC, Grey High Gloss 4:1 Two Component Epoxy.  The coating is packaged in a kit form, with Part 1 and Part 2 with premeasured amounts.

- Reduction - paint may be reduced using SP05127T0 Epoxy Reducer

  - 0 - 10% for airless spray

  - 0 - 15% for air assist airless spray

  - 10 - 20% for air spray

  - 0 - 5% for brushing

- Apply the mixed coating in two coats to insure proper film build.

- Allow the coating to cure 16 hours at room temperature before shipping outside.

  - Top coating - the tank is now ready for top coating using SP04001I1/SP03937P2 Grey High Gloss 9:1 Urethane.  The coating is packaged in a kit form with Part 1 and Part 2 supplied ready to mix.

  - Topcoat Reduction - depending on the type of equipment being used to apply coating it will require thinning as follows with SP01174T0 reducer.

    - 0 - 10% for airless spray.

    - 0 - 15% for air assist air less spray.

    - 10 - 20% for air spray

- Apply the mixed coating in two thin coats to insure proper film builds.

- Allow the coating to cure 8 hours at room temperature before shipping outside.