EPL 1200 SERIES PLANTER BAR

## QUALITY ASSURANCE PROCEDURE

# Attachments:  Planter Bar Series Q.A. Checklist

Pretreatment/Cure Testing Diagram

Mil Testing Diagram

Hatch & MEK Testing Diagram

References:  PLS 802  Pretreatment Quality Assurance Procedure

PLS 205 Powder Paint Cure Quality Assurance Procedure

This procedure explains and outlines the quality assurance checks for the Planter Bar Series

Responsibilities are as follows:

- The Pretreatment Operator is responsible to:

- Record on the Planter Bar Series Q.A. checklist

i) Name, Date and Time

ii) Pretreatment conditions (within 1.5 hours of the Pivot Toolbar being

pretreated in the wash)

iii) Water Break Test result

iv) Take the checklist to the painters as soon as possible

- The Painters are responsible to:

- Receive the Planter Bar Series Q.A. checklist from the pretreatment operator

- Perform and document the following testing (all locations of testing must be documented on attached diagram)

i) White Rag Test

ii) Phosphate Test using Test Solution #47

iii) Flash Rust N/C

iv) Chemical Run N/C

Note: i) and ii) are to be done on the first planter bar of each shift while

iii) and iv) are to be checked on all parts on the line randomly

throughout the day

- Document the following:

i) Painted by (indicate both east and west side painter employee

numbers)

ii) Cure conditions (oven temp., track speed and any non

conformances)

iii) Initiate and document the planter bar ID #s

iv) Circle if it is a rigid bar or trailing arm

3)    Place the magnetic temperature gauge on the hottest part of the planter bar.

When the temp. on the gauge reads 100*F or less, then you may start to

take mil readings. Any mil readings taken above this temp. may result in

damage to the probe.

Perform and document the following inspections/testing:

i)  Pinhole Classification (visual inspection based on Powder Paint

Cure Quality Assurance Specification)

ii) Gloss Rating (visual inspection based on Powder Paint

Cure Quality Assurance Specification)

iii) Mil Thickness (document mils on appropriate diagram with min.

max. and avg. on checklist)

NOTE: Ensure gauge is calibrated properly using an 11 gauge panel

That has been blasted and washed within 5 days.

iv) Hatch Test Results (locations as per diagram and performed as

per Powder Paint Cure Quality Assurance Specification)

v) MEK Test Results (locations as per diagram and performed as

per Powder Paint Cure Quality Assurance Specification)

vi) Paint Non Conformance (note any contamination, etc.)

- Document for repaint

i) circle ‘yes’ or ‘no’

ii) if ‘yes’, document reason for repaint, complete appropriate repairs as per repaint standards and		 document in Repaint Record section on checklist

- Inspected by . . . sign it (painter/inspector)

- Touch up Hatch & MEK test marks with 5:1 urethane paint that has been catalyzed

- The planter bar must be signed off as good and passing all inspections/testing by the Supervisor or designate.

f)   Sticker the planter bar with ID #s and put checklist with planter bar for release to assembly.

Planter Bar Quality Assurance Checklist

Date:  __________________________                                  Time: _______________am / pm

Sequence Number: _______________                                   Rigid / Trailing Arm

PRETREATMENT

Wash Operator: __________________                                 Employee ID#: ______________

PREATREATMENT CONDITIONS

Inproclean 1300        H2O Rinse               Cryscoat 547C           H2O Rinse               H2O Rinse

%: ______             %: ______               %: ______                %: _______              %: _______

pH: ______            pH: ______             pH: ______               pH: _______            pH: _______        temp: ______ C     temp: ______C        temp: ______C         temp: _______C      temp: _______C

psi: ______            psi:  ______             psi: ______               psi: _______            psi: _______

tds: _______                                              tds: _______            tds: _______

PRETREATMENT TESTING

Water break (visual):  _________  Comments:  ________________________________________

Phosphate (T.S. #47): _________  Comments:  ________________________________________

White rag test :           _________  Comments:  ________________________________________

Flash rust N/C :          ____________________________________________________________

Chemical run N/C:     ____________________________________________________________

(All testing locations to be documented on appropriate diagram.)

PAINT

Painted by: (east) _____________________   Employee ID#: ________________

Painted by: (west) _____________________  Employee ID#: ________________

CURE CONDITIONS

Oven Temp: ______________                         Track Speed: ____________ft/min.

Comments:  ____________________________________________________________________

CURE TESTING

Pinholes Classification:  ___________                    Paint Mils:

Hatch Test Result:          ___________                    Minimum:  ______________

MEK Test Result:           ___________                    Maximum:  ______________

Gloss Rating:                   ___________                   Average:     ______________

Paint non-conformance: __________________________________________________________

______________________________________________________________________________

Repaint:    NO

YES          Reason:  _____________________________________________________

Inspection by: ___________________________          Employee ID#:  _____________________

Signed off by: ___________________________	         Employee ID#:  _____________________

REPAINT RECORD

Area(s) repainted:  _______________________________________________________________

Reason:  _______________________________________________________________________

Description of work:  ____________________________________________________________

Rechecked/ signed off by:  ________________________  Employee ID#:  __________________

Time/Date Started:    ________________________

Time/Date Finished:  ________________________

Total Time to Fix:      ________________________

PLANTER BAR HATCH & MEK LOCATIONS

### PLANTER BAR MIL TESTING LOCATIONS

PLANTER BAR PRETREATMENT TEST LOCATIONS

W - White Rag Test

F   - Flash Rust

C  - Chemical Run

P   - Phosphate Test

### PLANTER BAR MIL TESTS

Low: _____

High: _____

Avg.: _____

# Text boxes

Hatch & MEK

(between plates)

Hatch & MEK (inside)

4

3

2

1

5

6

11

10

9

12

8

7

12

11

10

9

8

7

6

5

4

3

2

1